Document Title:

Ceramic Substrate Prototype Specification

Client Use Case

The client requires a ceramic-based PCB prototype suitable for

high-temperature operation in a power electronics module.

Key Requirements

- Operating temperature: up to 220°C

- Continuous current: 30A

- Copper thickness: 300 µm

- Substrate material: Aluminum Nitride (preferred)

- Dielectric strength: minimum 20 kV/mm

Mechanical Constraints

- Board dimensions: 80 mm x 60 mm

- Maximum warpage: < 50 µm

- Mounting holes: 4x M3

Prototyping Notes

Low-volume prototyping (5–10 units) is required for initial validation.

Design files will be supplied as Gerber and DXF formats.

Open Questions

- Feasibility of via-in-ceramic technology

- Lead time for AlN substrate sourcing

- Cost implications for small batch production